Malatya (Turkiye) Pb-Zn Cevherleşmelerinin Eski İmalat Pasalarının Jeokimyası

Leyla Kalender, Güllü Kırat, Cemal Bölücek & Ahmet Sağıroğlu

Fırat Universitesi, Jeoloji Mühendisliği Bölümü, 23119 Elazığ (E-posta: leylakalender@firat.edu.tr)

İnceleme alanı, Malatya İlinin Yeşilyurt ilçesine bağlı Görgü köyünün 9 km kuzeydoğusunda ve 1/25000 ölçekli Malatya L40-a4 paftasında yer almaktadır.

Görgü (Cafana) Pb-Zn cevherleşmesi, volkanitler (yaş?) ile Malatya metamorfitleri (Permo(Karbonifer) içerisinde gelişmiş olup cevherleşmenin büyük bir kısmı andezitik kayaçlar içerisinde damar şeklindedir.

Sülfür cevherleşmesi olarak gözlenen cevherleşmenin ana mineralleri galen, sfalerit, pirit, markasit, simitsonit, zinkit, hidro-zinkit, anglezit ve seruzit; gang mineralleri ise barit, dolomit, kuvars ve kalsittir.

Bu çalışmada, ana yatak cıvarından 12 adet pasa ve 18 adet sistematik toprak örneği alınarak, örneklerinin metal içerikleri ve metallerin birbirleri ile olan ilişkileri incelenmiştir. Pasa örneklerinde ortalama Pb (6259,39 ppm ±3937), Zn (6618,28 ppm ±3725), Ag (3711 ppb ±5180), Mn (829 ppm ±850), Ba (546,4 ppm ± 475); toprak örneklerinde ise Pb (663 ppm ±2332), Zn (660 ppm ±2107), Ag (64,06 ppb ±30), Mn (993 ppm ±331) ve Ba (276 ppm ±287) içeriği tespit edilmiştir. Toprak ve pasalardaki ortalama metal içerikleri karşılaştırılmış ve topraktaki Au, Mn, Sn, Cu, Sb, Rb ve Sr değerlerininin doğal ayrışma nedeniyle pasalardan daha fazla olduğu belirlenmiştir.

Veri sayısı az olduğu icin pasa orneklerinde spearman korelasyon katsayıları hesaplanmıstır. Bu verilere gore, Ag, Pb, Zn, Cu, Mn, Mo, Sn ve Hg’ nın; Sr, Ba, Rb, Ce, Cs, La, U, Se, Sb ve Cd (LIL: large ion lithophile) ile pozitif, aynı metallerin Sc, V, Y, Nb, Th ve Ti (HFS: High field strength) ile negatif iliski sunduğu belirlenmistir. Bu durum, cevherlesmeyi olusturan hidrotermal cozeltilerde kıtasal kirlenmenin etkili olduğunu gostermektedir.

Anahtar Sözcükler: Görgü Pb-Zn cevherleşmeleri, jeokimya, pasa, toprak kirliliği

Geochemistry of Waste at Pb-Zn Görgü Mine, Malatya, Turkey

Leyla Kalender, Güllü Kırat, Cemal Bölücek & Ahmet Sağıroğlu

Fırat Universitesi, Jeoloji Mühendisliği Bölümü, TR(23119 Elazığ, Türkiye

(E-mail: leylakalender@firat.edu.tr)

The study area is located at section Malatya L40-a4 of 1/25000 scale map in the 9 km northeast of Görgü villiage of Yeşilyurt township in Malatya.

The Görgü (Cafana) Pb-Zn mineralization forms in volcanic rocks (age ?) and Malatya metamorphic rocks (Permo(Carboniferous) and the great deal of mineralization take place in andesitic rocks as vein forming. The Pb-Zn mineralizations have been observed as sulphur minerals. Major minerals are galena, sphalerite, pyrite-marcasite, smithsonite (the dominant ore mineral), zincite, hydro-zincite, anglesite, cerussite and gangue minerals are represented barite, dolomite, quartz and calcite.

In this study, 12 mine waste samples and 18 soil samples were collected from within mine waste piles and around of ore deposits, determined concentrations and distribution of the metals. In the mine wastes and soil samples were estimated average and standard deviation values and Pb (ppm 6259,39 ±3937), Zn (ppm 6618,28 ±3725), Ag (ppb 3711 ±5180), Mn (ppm 829 ±850), Ba (ppm 546,4 ±475); Pb (663 ppm ±2332), Zn (660 ppm ±2107), Ag (64,06 ppb ±30), Mn (993 ppm ±331) ve Ba (276 ppm ±287), respectively. Correlate to element concentrations between waste and soil show that Au, Mn, Sn, Cu, Sb, Rb and Sr values in soil are higher than waste due to natural weathering processes.

Spearman correlation coefficients were evaluated because data were insufficient. According these values, between Ag, Pb, Zn, Cu, Mn, Mo, Sn, Hg and Sr, Ba, Rb, Ce, Cs, La, U, Se, Sb, Cd (LIL) correlation coefficients are positive. However, between Ag, Pb, Zn, Cu, Mn, Mo, Sn, Hg and Sc, V, Y, Nb, Th, Ti (HFS) correlation coefficients are negative. It is suggested that the ore forming hydrothermal fluids may be affected by crust contamination.

Key Words: Görgü Pb-Zn mineralizations, geochemistry, mine waste, soil pollution